## Slide 1: Bioinspired DNA origami capsids
S. Fraden1, G. Grason2, R. Hayward2, M. Hagan1, W. Rogers1, C. Santangelo2,
H. Dietz3, 1Brandeis University, 2U. Mass. Amherst, 3Tech. Universität München
DMR MRSEC 1420382
2019
(A) Structures of icosahedral virus capsids, where T is the number of distinct local symmetry environments (indicated by color). (B) Cryo-electron microscopy reconstructions of DNA origami capsids. (C) (right) TEM tomogram of an origami capsid assembled around a DNA molecule labeled with gold nanoparticles. (left) Schematic of the structure. (D) Prediction of the yield T=3 capsid yield as a function of subunit-subunit interaction strengths that drive dimer formation () and pentamer formation (), from Langevin Dynamic simulations.
DNA origami technology is used to develop building blocks that self-assemble into predetermined finite-sized structures. The objectives of this research are to understand, control, and build self-closing structures inspired by self-assembling viruses, whose smallest capsids have an icosahedral symmetry and are decomposable into so-called “quasi-equivalent” triangular subunit arrangements, characterized by the “T” number (Fig. 1A). Assembly occurs using programmed edge-edge interactions based on a lock-and-key mechanism and base stacking between the blunt ends of the double-helices. Researchers have successfully designed, assembled and characterized capsids of octahedral and icosahedral symmetry, including T1, T3, T4, and T9, and studied the determinants of capsid assembly experimentally and with a direct comparison to a computational model to test how the kinetics and yield of target structures depends on control parameters and assembly pathways (Fig. 1).
Notes: Include a technical description of the work here in the Notes section.