## Slide 1: Self-Regulated Non-Reciprocal Motions in Liquid Crystal Elastomer Pillars
Living cilia stir, sweep, and steer via swirling strokes of complex bending and twisting paired with distinct reverse arcs. Efforts to mimic their dynamics rely on multi-material designs, since programming arbitrary motion is difficult in single materials.
A team at the Harvard MRSEC led by Bertoldi and Aizenberg has developed an approach to achieve a diverse trajectories from a single-material system via self-regulation: when a photoresponsive liquid crystal elastomeric pillar with mesogen alignment is exposed to light, it ‘dances’ dynamically as light initiates a traveling order-to-disorder transition front that twists and bends via opto-chemo-mechanical feedback. Guided by a theoretical model, a wide range of trajectories are realized by tailoring light illumination, molecular anisotropy, and geometry. Furthermore, higher order dynamics emerge in micro-pillar arrays and jointed geometries, with broad implications for autonomous actuators used in soft robotics, biomedical devices, and energy transduction materials.
Joanna Aizenberg (Chem and MatSci) and Katia Bertoldi (MechE)
(A) Design principle to achieve diverse deformation trajectories: misalignment of molecular anisotropy (M), microstructure geometry (G), and light (L). (B) Formation of a transient propagating bimorph in a single material by directional light-activation with a stationary light source. (C) Upon irradiation from opposite sides, the same microstructure displays mirrored right- and left-handed curved stroke-like trajectories, which are captured by FE modeling. (D) Spontaneous self-organization of strings of microposts into an undulating line. Modeling results on the right. (E) Simulation and experimental results of X-shaped jointed compositionally uniform microactuators exhibit twisting/rotation of the stem and amplified sway motion of the horizontal arms.
Three non-colinear axes
trans-
cis-
A
B
UV off
UV on
50 μm
Self-sorting
Mirrored stroke
Jointed microactuators
C
D
E
Transient propagating bimorph
FE
S. Li, M.M. Lerch, J.T. Waters, D. Deng,R.S. Martens, Y. Yao, D. Kim, K. Bertoldi, A. Grinthal, A.C. Balazs, and J. Aizenberg, “Self-regulated non-reciprocal motions in single-material microstructures”, Nature (accepted Feb. 2022).
2021-2022
Harvard MRSEC
DMR 2011754
Notes: A team at the Harvard MRSEC led by Bertoldi and Aizenberg has developed an approach to achieve a diverse trajectories from a single-material system via self-regulation: when a photoresponsive liquid crystal elastomeric pillar with mesogen alignment is exposed to light, it ‘dances’ dynamically as light initiates a traveling order-to-disorder transition front that twists and bends via opto-chemo-mechanical feedback. Guided by a theoretical model, a wide range of trajectories are realized by tailoring light illumination, molecular anisotropy, and geometry.
This work was funded in part by the Harvard MRSEC and recently accepted for publication:
Li, S.*, M.M. Lerch*, J.T. Waters, B. Deng, R.S. Martens, Y. Yao, D. Kim, K. Bertoldi, A. Grinthal, A.C. Balazs, and J. Aizenberg, “Self-regulated non-reciprocal motions in single-material microstructures,” Nature (accepted Feb 2022).