## Slide 1: Discovery of a hexagonal easy-plane metallic antiferromagnet in the CuMnAs system
D. P. Shoemaker and A. Schleife
University of Illinois Urbana–Champaign
Illinois MRSEC
DMR-1720633
2020
We discovered a new hexagonal metallic antiferromagnetic phase in the Cu-Mn-As system. Electrical switching and read-out of tetragonal CuMnAs inspired a world-wide research effort in metallic antiferromagnets. Phase equilibria in this system (Fig. a) however is poorly understood.
We synthesized crystals of hexagonal Cu0.8Mn1.2As and determined their chemical (Fig. b) and magnetic structure (Fig. c) through X-ray and neutron scattering supported by first principles density functional theory. No previously-known material of any composition has the same arrangement of atoms, so our work creates new possibilities for designing and engineering materials.
Conclusion: The discovery of new metallic antiferromagnetic phases advances fundamental understanding of this important new class of materials.
Cu0.8Mn1.2As
a)
b)
c)
M. Karigerasi et al., Phys. Rev. Mat. 3, 111402(R) (2019)
Notes: A key goal of IRG1 is to discover new antiferromagnetic materials that exhibit high Néel temperatures and are susceptible to spin manipulation by optical and electronic stimuli. The challenge is to find and develop materials with the desired symmetry, metallic conductivity, and magnetic anisotropy. Shoemaker discovered a new hexagonal metallic antiferromagnetic phase in the Cu-Mn-As system and solved the magnetic structure of h-Cu0.8Mn1.2As. The spin structure is shown in the bottom right figure. No previously-known material of any composition has the same arrangement of atoms. The arrangements of the in-plane moments in of h-Cu0.8Mn1.2As was investigated through a combination of neutron diffraction by Shoemaker and density-functional-theory by Schleife.