## Slide 1
An NSF Materials Research Science and Engineering Center (MRSEC)
Supported under Award Number DMR-0820414
Strain tunable room temperature magnetism
Center for Emergent Materials
The Ohio State University
Co Au Co
The properties of epitaxial Sr2CrReO6 films shows remarkable substrate dependence
The presence of strong spin–orbit coupling in oxides containing 5d transition metal ions provides a mechanism for direct coupling between magnetization and the crystal lattice. In epitaxial films of such compounds strain arising from lattice mismatch with the substrate can in principle be used to tune the magnetic properties.
Using a novel deposition technique, IRG-2 researchers have grown fully-ordered Sr2CrReO6 films which are semiconducting and highly magnetic at room temperature. When grown on different substrates dramatic changes in magnetization and resistivity occur. The largest effects are seen when Sr2CrReO6 is grown on Sr2GaTaO6 buffer layers (1.6% tensile strain) where the low temperature resistivity increases by more than two orders of magnitude, and the saturation magnetization more than doubles, with respect to films grown on a lattice matched substrate (e.g. SrTiO3). Electron microscopy images suggest that changes in the local atomic structure may be responsible for the change in properties (see the zig-zag columns of Re on the right). This effect could potentially be exploited in a variety of ways, including strain sensors and magnetoelectric composite films.
http://cem.osu.edu
Hauser, Williams, Dixit, Soliz, Susner, Sumption, Fraser, Woodward, Yang (unpublished)
Sr2CrReO6 on SrTiO3
Almost perfect lattice match and clear ordering of Re/Sr/Cr atoms
  Sr2CrReO6 is a semiconductor, not a metal as previously believed
Record high saturation magnetization of 1.38 μB per formula unit for Sr2CrReO6
  confirm strong spin-orbit coupling
Sr2CrReO6 on Sr2GaTaO6
Lattice mismatch of +1.6% and zig-zag pattern of atomic columns
  Sr2GaTaO6 buffer layer greatly reduced interfacial defects in Sr2CrReO6.
Greatly enhanced magnetization: 3.28 μB/f.u. (a factor of 2.4) compared to films grown on SrTiO3
Scanning Transmission Electron Microscopy (STEM) images
Notes: Sr2CrReO6 epitaxial films were grown on a number of substrates and buffer layers by off-axis magnetron sputtering in an ultrahigh vacuum sputtering system with a base pressure of 5 × 10−10 Torr. The substrates/buffer layers cover a range of lattice mismatch with the films, including SrTiO3 (−0.1% compressive strain), LSAT (−0.9% compressive strain), strained Sr2CrNbO6 buffer layer (−0.1% compressive strain) on SrTiO3, and Sr2GaTaO6 (+1.6% tensile strain). The structural and magnetic properties of the Sr2CrReO6 films were characterized by several techniques, including triple-axis x-ray diffraction, four-probe transport and vibrating sample magnetometry measurements using a Physical Property Measurement System in a magnetic field up to 14 T and temperatures down to 2 K. X-ray diffraction scans of the Sr2CrReO6 films grown on SrTiO3 show pronounced Laue oscillations and narrow rocking curve with FWHM of 0.0066, indicating high crystalline quality. Resistivity and magnetization of the Sr2CrReO6 films exhibit dramatic strain dependence. Scanning Transmission Electron Microscopy (STEM) images show a high degree of Cr/Re ordering on SrTiO3 and a clear zig-zag bending of the atomic columns on Sr2GaTaO6. The links between magnetization and the atomic structure are under investigation.