## Slide 1
IRG-3: Single Photon Bound States in Microwave Photonic Crystals (DMR-1420541) Andrew Houck, Princeton University
Creating a microwave photonic bandgap. A microwave photonic bandgap is created by periodically modulating impedance along the length of a transmission line, achieved by changing the width and gap sizes of the coplanar waveguide. A single qubit is strongly coupled to one of the bands in this transmission line photonic crystal. This system has been predicted to realize single photon bound states, which can be used to probe and manipulate interacting quantum systems.
Evidence for a single photon bound state in a photonic bandgap medium. A qubit is tuned through the band edge while monitoring transmission through the system. An avoided crossing with the band edge, and the emergence of a defect state in the bandgap when the qubit is tuned above the band edge, are evidence for sthe existence of single photon bound states.
Reference: Yanbing Liu and Andrew Houck, “Quantum Electrodynamics Near a Photonic Bandgap,” arXiv:1603.02998, Submitted (2016).
Photonic crystals provide an extremely powerful toolset for manipulation of optical dispersion and density of states. The unique control afforded by these media make them a beautiful, if unexplored, playground for strong coupling quantum electrodynamics, where a single, highly nonlinear emitter hybridizes with the band structure of the crystal. In this work we demonstrate that such hybridization can create localized cavity modes that live within the photonic band-gap, whose localization and spectral properties we explore in detail. We then demonstrate that the colored vacuum of the photonic crystal can be employed for efficient dissipative state preparation. This work opens exciting prospects for engineering long-range spin models in the circuit QED architecture, as well as new opportunities for dissipative quantum state engineering. Moreover, this cavity structure is a promising platform for controlling and measuring high coherence quantum spin systems.
Notes: Abstract: We employ a fluorescence bilayer method to directly measure the glass transition temperature (Tg) of the irreversibly adsorbed layer of polystyrene (PS) buried in bulk films as a function of adsorption time, tads. This bilayer geometry allows for the examination of interfacial effects on Tg of the adsorbed nanolayer. In the presence of a free surface, we observe a substantial reduction in Tg from bulk that lessens with tads as a result of increased chain adsorption at the substrate. Submerging the adsorbed layer and effectively removing the free surface results in a suppression of the Tg deviation at early tads, suggesting chain adsorption dictates Tg at long tads. Annealing in the bilayer geometry promotes recovery of bulk Tg on a timescale reflecting the degree of adsorption. Our data are quantitatively rationalized via the Free Volume Holes Diffusion model, which explains adsorbed nanolayer Tg in terms of the diffusion of free volume pockets towards interfacial sinks.

## Slide 2: Photonic bound states with qubit in filter