## Slide 1: Electrically-Fueled Active Materials
Figure 1. Fluorescence snapshots showing directional fiber growth when current was applied (green square), and dissolution when current was turned off (red square), scale bar = 50 µm.
DMR-2011967, MRSEC
2022 IRG-2 Intellectual Merit
S. Selmani, E. Schwartz, J. T. Mulvey, A. Grosvirt-Dramen, W. Gibson, A. I. Hochbaum, J. P. Patterson, R. Ragan, Z. Guan (University of California, Irvine)
Dissipative Self-Assembly
Fuel-driven self-assembly is ubiquitous in natural systems, leading to complex phenomena including cell motility, cell division, camouflage, and self-healing. Creating synthetic equivalents of these biological assemblies is challenging but offers the reward of active, dynamic materials.
Electrically-Fueled Assembly
Current synthetic dissipative self-assembly systems are fueled either by chemicals or light. Here, the UCI MRSEC team have developed the first electrically-fueled dissipative system that offers rapid kinetics, directionality, and unprecedented spatiotemporal control, closely mimicking systems found in nature. The electrochemically-fueled active, dynamic, and directional assembly is shown in Figure 1. Excitingly, the system demonstrates an unprecedented level of spatiotemporal control of self-assembly (Figure 2).
The team is now working on expanding this chemistry to a completely waste-free dissipative system. The transient behavior of dissipative self-assembly using dual electrocatalysts without generating any waste has been preliminarily demonstrated (Figure 3).
Selmani S, Schwartz E, Mulvey J, Wei H, Grosvirt-Dramen A, Gibson W, Hochbaum AI, Ragan R, Patterson J, Guan Z,* “Electrically fueled active supramolecular materials” Journal of American Chemical Society, 144, 7844-7851 (2022). https://doi.org/10.1021/jacs.2c01884
Figure 2. Controlled growth and disassembly at individually addressable electrodes demonstrating unprecedented spatiotemporal control over dissipative self-assembly.
0′
10′′
20′
20′10′′
40′
40′10′′
60′
Figure 3. Fluorescence snapshots showing fiber growth under voltage (green square) and dissolution when voltage is turned off (red square), scale bar = 100 µm.