## Slide 1
Photoinduced Morphology Change in Ionically Compatibilized Copolymer
UC Santa Barbara MRSEC
DMR 2308708
Javier Read de Alaniz and Rachel Segalman (UC Santa Barbara)
‡Karnaukh, ‡Xie, Yang, Komal, Segalman*, Read de Alaniz*, Photoinduced morphology change in ionic supramolecular block copolymer, J. Polym. Chem. 15 (2024) 3806–3813. DOI: 10.1039/d4py00682h
Scheme of the photoinduced HEX-to-LAM transition in a PS/PDMS ionic blend, driven by ion association changes upon photochromic end-group isomerization.
Previously, UC Santa Barbara MRSEC researchers demonstrated that chain-end functionalization of immiscible polystyrene/polydimethylsiloxane (PS/PDMS) blends with oppositely paired acid and base groups forms ionic supramolecular block copolymers, where electrostatically stabilized microdomains prevent macroscopic phase separation.
In this work, we developed a facile strategy to dynamically tune ionic interactions through light irradiation, enabling morphological transitions within a single polymer blend by post-functionalizing PDMS with a photochromic end-group.
Photoisomerization increases the local positive charge, strengthening ionic bonds between dissimilar blocks while enhancing repulsion between adjacent groups. This electrostatic repulsion expands the interfacial area per polymer chain, driving a HEX-to-LAM a phase transition.
By leveraging controllable end-group photochemistry, this methodology can enable the construction of microstructured functional polymeric materials with a wide tunability window.
Notes: What Has Been Achieved: Please see above.
Importance of the Achievement: By leveraging controllable end-group photochemistry, this methodology can enable the construction of microstructured functional polymeric materials with a wide tunability window.
How is the achievement related to the IRG, and how does it help it achieve its goals? An important goal of IRG-1 is to develop new and more sustainable polymers for a variety of applications.
Where the findings are published: ‡Karnaukh, ‡Xie, Yang, Komal, Segalman*, Read de Alaniz*, Photoinduced morphology change in ionic supramolecular block copolymer, Polym. Chem. 15 (2024) 3806.
DOI: 10.1039/d4py00682h