## Slide 1: Computational Design of Tetrahelical Peptide Bundle Variants Spanning a Wide Range of Charge States
Research Focus
A homotetrameric helical bundle was computationally designed to have a variety of net charges.
The charged bundle variants showcase how charge state can be controlled for a common peptide structure, as well as the properties of the fibril nanomaterials constructed by the peptide building blocks.
Key Advances
A probabilistic peptide design algorithm was applied to identify peptide sequences with putative charge states spanning -8 to +8 for a tetrahelical backbone.
The peptides folded as designed despite the drastic variation of exterior charges, confirmed by experimental studies: circular dichroism, analytical ultracentrifugation, and small-angle neutron scattering spectra.
Highly negative peptides (sequence net charge from -8 to -4) were less thermally stable with lower melting temperatures.
One dimensional nanofibrils constructed by positive peptides and negative peptides showed different morphologies under transmission electron microscopy.
January 20, 2022
Interdisciplinary Research Group (IRG): [Peptide Active Materials (PAMs)]
Highlight Authors:
R. Guo (University of Pennsylvania), N. Sinha, R. Misra, C. Kloxin, G. Jensen, D. Pochan (University of Delaware), J. Saven (University of Pennsylvania) [University of Delaware MRSEC DMR-2011824]
For more Information: https://doi.org/10.1021/acs.biomac.1c01539
IRG 1
Figure: Electrostatic surface renderings of tetrahelical peptide bundles. The net charge of a single helix labeled above (first row) and below (second row) each peptide, the putative charge of the entire bundle is four times the indicated charge. Electrostatic potentials are colored on a red (negative) – white (neutral) – blue (positive) scale.
-8
-7
-6
-5
-4
-3
-2
-1
+8
+7
+6
+5
+4
+3
+2
+1
Notes: Further explanation: This article, recently published in Biomacromolecules 2022 23 (4), 1652-1661, results from MRSEC supported research through a collaboration between IRG1 groups Saven, Pochan, and Kloxin (3 MRSEC faculty primary participants). The study used the MRSEC-supported facility.