## Slide 1
Complementary Methods for Characterizing Excitations in Hybrid Materials
Figure 1. a) Schematic of instrument enabling ultrafast THz emission, absorption, and pump-probe experiments. b) Temporal evolution of THz emission from a FeGaB/BiSb thin film for two opposite magnetization directions. c) Micro-focused BLS system. d) Schematic illustration of the Stokes process in which a magnon is created. e) Thermal spin-wave spectrum from a FeGaB/BiSb thin film.
May 12, 2021
UD CHARM DMR-2011824
The UD MRSEC team is developing and employing a suite of novel experimental characterization techniques that provide important insights into hybrid materials, in which unique properties arise due to interactions between material constituents. The team recently characterized a ferromagnet/topological insulator hybrid material using both ultrafast THz spectroscopy and Brillouin Light Scattering (BLS), which allowed the team to measure both 1) the THz radiation emitted as a result of spin-to-charge conversion, and 2) the thermal spin waves in the constituent materials.
Authors with Affiliation(s): Gundlach, Jungfleisch, University of Delaware
IRG Group Number: 2
Related Research Group(s): Hybrid Quantum Materials with Emergent Terahertz Functionalities (HQ-METs)
Notes: Pump-probe time-resolved THz spectroscopy is one of the key techniques for measuring THz excitations in novel hybrid quantum materials. Panel a depicts the new laser instrument that enables versatile ultrafast THz emission, absorption, and pump-probe experiments. Panel b shows a time-resolved measurement of the electric field transient (i.e. the THz pulse) resulting from optical excitation of a FeGaB/BiSb thin film bilayer hybrid material. The sign of the THz electric field is reversed for two opposite directions of the magnetization in the FeGaB constituent (data not yet published). Panel c shows a schematic depiction of the micro-focused Brillouin Light Scattering (BLS) instrument, including the optical path of both the incident and reflected laser beams. Image adapted from T. Sebastian et al., Front. Phys. 3, 1589 (2015). Panel d schematically illustrates the Stokes BLS process, in which a magnon is created. Energy and momentum conversation result in a reduced wavevector kS and decreased frequency ωS of the scattered light, which is measured to deduce the frequency of the magnons that are created. Image adapted from M. B. Jungfleisch – Inelastic scattering of light by spin waves in “Optomagnonic structures” by. E. Almpanis, World Scientific (2021). Panel e shows the thermal spin-wave spectrum from the FeGaB/BiSb bilayer hybrid material as measured with BLS (data not yet published). These data demonstrate how complementary characterization methods can provide important insights into what is happening within a hybrid material (e.g. the thermal spin waves) that influences the resulting THz emission.