## Slide 1
Support: Primary NSF MRSEC DMR-11-20901
In the past few years, the theory of topological band structures has been generalized beyond topological insulators to include topological semimetals, including Weyl semimetals, Dirac semimetals and other “symmetry protected” topological states. HgTe is a semimetal in which the degeneracy of the conduction and valence band at the G point is protected by symmetry. In their early work on topological insulators, Fu and Kane showed that straining HgTe opens a gap at G, resulting in a topological insulator. Here we showed that the situation in HgTe is a bit more complicated – and interesting. For tensile strain, while the degeneracy at G is lifted, away from G bands must cross the Fermi energy, resulting in an unusual kind of Fermi surface that is protected by mirror symmetry and features doubly degenerate bands that cross two singly degenerate bands. The band crossing is neither a Weyl point (a singly degenerate crossing) nor a Dirac point (a doubly degenerate crossing), but rather a hybrid between the two. This leads to a nontrivial texture for the electronic spin on the Fermi surface. We combined first principles calculation with a systematic k·p analysis to map out these properties in detail.
Topological Semimetal in Tensile Strained HgTe
C.L. Kane, E.J. Mele and A.M. Rappe
Spin Texture on the Fermi Surface of a Toplogical semimetal:
Top left: Band dispersion in the k·p theory of strained HgTe as a function of momentum along the (111) axis, featuring an unusual band crossing. The Fermi surface (bottom left) consists of two spherical shells that touch on the z axis. The right panels show the spin texture and spin winding numbers of the valence band states on the red (blue) Fermi surfaces. There are three points indicated where the spin texture vanishes.
Notes: We carried out ab initio and k·p calculations of the spin texture on the Fermi surface of tensile strained HgTe, a material obtained by stretching the zincblende lattice along the (111) axis. We find that its Fermi surface consists of two ellipsoids which contact at the point where the Fermi level crosses the two-fold degenerate band along the (111) axis. However, a topological analysis of the spin texture of its bands shows that neither ellipsoid carries a compensating Chern number. Consequently, the spin texture is locked in the plane perpendicular to the (111) axis with a nonzero winding number in that plane that changes from one end of the Fermi ellipsoids to the other. This change in the winding number reveals the existence of singular points in the spin texture on its Fermi surface. We carried out ab initio calculations of Hg½Zn½Te, where chemical substitution induces tensile strain and confirmed the existence of a spin texture locked in a 2D plane on the Fermi surface with different winding numbers on either end.