## Slide 1: Shewanella oneidensis as a Living Electrode for Controlled Radical Polymerization
N. A. Lynd, B. K. Keitz: University of Texas at Austin
MRSEC: DMR-1720595
Metabolic engineering produces fuels, pharmaceuticals, and materials using microbial catalysts. We sought to expand the power of these catalysts by redirecting respiratory electron flux from Shewanella oneidensis to a metal polymerization catalyst.
Our microbial polymerization features characteristics of controlled radical polymerization such as first-order kinetics, narrow molecular weight distributions and block-copolymer synthesis. Catalyst performance and polymer microstructure were a strong function of bacterial metabolism, specific electron transport proteins, and catalyst design.
Overall, our results suggest that manipulating biological electron transport pathways may be a general strategy for allowing bacteria to produce or communicate with synthetic materials.
Scheme 1. (a) Electron equivalents generated from S. oneidensis MR-1 reduce a metal catalyst from an inactive state (MOX) to an active state (MRED) to enable ATRP, (b) molecular weight and polydispersity of poly(OEOMA500) as a function of monomer conversion, (c) rescue of normal polymerization activity via knockout complementation with a plasmid encoding MtrC.
2018
G. Fan, C. M. Dundas, A. J. Graham, N. A. Lynd, and B. K. Keitz, PNAS DOI:10.1073/pnas.1800869115 (2018).